## Slide 1: Nanoscale polarization transient gratings

## Slide 2: Research challenges
Interplay of charge, spin and lattice subsystems:
Properties ad functionality of solids, molecules and hybrid compounds
Transport phenomena
Collective excitations
Exotic nonequilibrium states & phase transitions
Extension to the XUV and X-ray regime:
chemical specificity
access to larger exchanged momentum and smaller length-scales.
Selectively investigate the time evolution of the different degrees of freedom via pump-probe techniques.
Introduction Transient Grating Polarization Grating Outlook
●○○○○ ○○○○○○ ○○○○○○ ○○○

## Slide 3: TG: a tool for probing collective dynamics
Sample
2θ
Strain grating (field-driven)
Elastic waves
(via electrostriction)
Intensity grating (Electronic excitations )
Molecular vibrations
Plasmons, polarons, excitons, etc.
Phonons, magnons, etc.
Polarization grating
Elastic waves (via thermal expansion)
“Magneto-elastic” coupling
Thermal grating
(heat diffusion)
Structural relaxations,
Heat waves, etc.
“pump 2” (k2,λFEL)
“pump 1” (k1,λFEL)
Circular Dichroism
This excitation is associated to a selected wavector ,
Introduction Transient Grating Polarization Grating Outlook
●●○○○ ○○○○○○ ○○○○○○ ○○○

## Slide 4: Extreme ultraviolet transient gratings
q ~ 0.1-1 nm-1
gap
TIMER’s (original) goal: fill the gap  probe collective lattice dynamics at ‘‘mesoscopic’’ scales (10’s nm)
[1] F. Bencivenga and C. Masciovecchio, NIMA (2009)
[3] F. Bencivenga et al., Advances in Phyisics; X 8, 2220363 (2023)
[2] F. Bencivenga et al., Faraday Discuss. 194, 283 (2016)
XUV probe
Kout
KEUV
KFEL1
KFEL2
Q
|Q|=4πsin(θ) / λFEL= 2π/ΛTG
EIS-TIMER beamline:
θ = 9.2o – 52.7o
λ > 60 – 4 nm
λpr = λ/3
ΔtF-F ≈ -1.7-7 ps (@52.7o)
|Q| ≈ 0.03-2.5 nm-1
ω up to ≈ 10 THz
The TIMER beamline is designed for a specific technique: EUV TG
Pro: Well defined scope and unique instrument worldwide!
Con: Well defined scope and unique instrument worldwide!
Introduction Transient Grating Polarization Grating Outlook
●●●○○ ○○○○○○ ○○○○○○ ○○○

## Slide 5: The EIS-TIMER instrument
Delay line: 4 ML mirrors tuned at the 3rd harmonic, time delay (Δt13) up to ns
fundamental harmonic (ω1)
Sample
Toroidal mirrors
3rd harmonic (ω3=3ω1)
Two plane mirrors (not shown)
2θ
The time delay (Δt11) between the two ω1 beams the can be varied in the -3 +7 ps range
θB
beam splitters
 | 20.8 nm | 16.6 nm | 13.3 nm | 8.34 nm
18.4o | 0.04 | 0.05 | 0.1 | 0.2
27.6o | 0.06 | 0.08 | 0.15 | 0.3
85o | 0.15 | 0.2 | 0.4 | 0.9
105.4o | 0.2 | 0.3 | 0.5 | 1.1
k-values (nm-1)
2θ
λ
~ 20 m long interferometer!
Introduction Transient Grating Polarization Grating Outlook
●●●●○ ○○○○○○ ○○○○○○ ○○○

## Slide 6: My FEL is (still) special 😝
e- bunch
Undulators
microbunching (growing from noise)
LINAC
simpler, higher brightness (similar to optical lasers), shorter wavelengths (up to hard x-rays), shorter time duration (a few fs)
SASE (LCLS, XFEL, etc.)
•••
•••
single longitudinal mode (high coherence), higher shot-to-shot stability, seed controls the output λFEL=λseed/N ; δtFEL=δtseed/N1/3
Seed laser
(λseed; δtseed)
Undulators
controlled microbunching
Modulator
Dispersive section
Seeded FEL emission
LINAC
•••
•••
e- bunch
Polarization: Variable linear and circular
Spectral purity: close to transform-limited
Tunable wavelength: 100 - 4 nm, 12 - 310 eV
High peak flux pulses: 50 - 100 fs, 1013 photons
FEL-optical jitter: < 10 fs (r.m.s.)
FERMI @ Elettra
Introduction Transient Grating Polarization Grating Outlook
●●●●● ○○○○○○ ○○○○○○ ○○○

## Slide 7: XUV-TG excitation mechanism
Space (x)
LTG
Space (x)
LTG
Space (x)
LTG
Space (x)
LTG
Review paper: L. Foglia et al., Photoacoustics 29, 100453 (2023)
Hot electrons
< 1 fs
e-e therm.
< 50 fs
Electron-lattice relaxation
< 1 ps
Lattice dynamics
hundreds of ps
Time (Δt)
Mean free path of excited electrons
 Fundamental periodicity limit
Introduction Transient Grating Polarization Grating Outlook
●●●●● ●○○○○○ ○○○○○○ ○○○

## Slide 8: Nanoscale thermoelasticity
Heat transport at the nanoscale is a hot area of research[1]
➔ thermal management of nanoelectronics, thermoelectric energy conversion, etc.
how fast is the thermal relaxation process at the nanoscale?
Characteristic dimensions of thermal gradient compare with phonon mean free path ➔ Fourier law of diffusion breaks down.
[1] M. Siemens et al., Nat. Materials 9, 26-30 (2010)
[2] Johnson et al., PRL 110, 025901 (2013)
τ-1 (GHz)
Q2 (μm-2)
~30 %
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●○○○○ ○○○○○○ ○○○

## Slide 9: Nanoscale thermoelasticity: Si
F. Bencivenga et al., Science Advances 5, aaw5805 (2019)
Review: L. Foglia et al., Photoacoustics 29, 100453 (2023)
Johnson et al., PRL 110, 025901 (2013)
Calculations by S. Hubermann (Mc Gill university)
Heat diffusion theory: predicts too short decay time (faster than heat carrier)
Phonon decay is known to be in the ns range ➔ cannot contribute to signal decay
Parameter free thermal transport model based on the Boltzmann equation ➔ Almost ballistic (decay time similar to acoustic period)
XTG can provide an experimental answer to the question!
τ-1 (GHz)
Q2 (μm-2)
Si 100nm ΛTG=69 nm
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●○○○ ○○○○○○ ○○○
Notes: Still not ballistic: too many phonon oscillations during thermal decay

## Slide 10: Surface elasticity
Sample manipulator (tilted sample)
Scattering plane
Detector
Folding mirror
Back-diffracted EUV TG signal
ω
2ω
    bulk STO ; LTG = 84 nm
Oscillation at ω ➔ thermal decay modulated by the SAW
Oscillation at 2ω ➔ “true” SAW decay
From waveform best fit ➔ extract the amplitude of the surface displacement (≈2 pm)
    Highest SAW ever excited (by an order of magnitude!) in any material: 50 GHz
    Possible to carry out experiments on bulk samples
    High frequency SAW may be also used to drive other dynamics (e.g. magnetoelasticity)
ω
2ω
A. A. Maznev et al., Appl. Phys. Lett., 119, 044102 2021
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●○○ ○○○○○○ ○○○

## Slide 11: Beyond thermoelasticity
    The TG signal is proportional to |Δn*|2
    In the EUV/X-ray regime n* is proportional to density
    Δn* ∝ Δρ/ρ ∝ ΔT (thermoelastic response)
    Co; ΛTG = 16.7 nm probe photon energy: ≈ 93 eV
    Co; ΛTG = 16.7 nm probe photon energy: ≈ 59 eV
The EUV probe is not sensitive to populations of electronic excited states, unless it is resonant with a core-hole transition
Probe diffracted by
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●○ ○○○○○○ ○○○

## Slide 12: Nanoscale magnetization gratings
Magnetic response
Thermoelastic response
Electronic response
[1] D. Ksenzov et al., Nano Lett. 21, 7, 2905–2911 (2021)
Probe (vertical polarization)
Detector for magnetic signal (only horizontal component)
Detector for the total signal (no polarizer)
ML mirror (polarizer)
Signal at resonance is dominated by magnetic response
Co0.81Gd0.19,
LTG = 44 nm
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ○○○○○○ ○○○

## Slide 13
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●○○○○○ ○○○

## Slide 14: Polarization Transient Gratings
2θ
y
x
2θ
y
x
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●○○○○ ○○○

## Slide 15
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●○○○ ○○○

## Slide 16: Polarization Transient Gratings
LV & LV
•••
•••
λseed
↕
↕
LV & LH
•••
•••
λseed
↕
↕
L. Foglia et al., Nature Commun. 15, 10742 (2024)
Intensity-grating: reflection signal is dominated by thermoelastic response!
Polarization Grating: Thermoelastic response scales & extra response appears (or is enhanced)!
Co0.78Gd0.22,
LTG = 44 nm
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●●○○ ○○○

## Slide 17: Excitation mechanism
M. Hennecke et al., Commun Phys. 7,191 (2024)
L. Foglia et al., Nature Commun. 15, 10742
Circular dichroism
controls the response to the excitation
Expect thermal responses to scale equally with
Emergent dynamics in polarization TG must originate from non-thermal modulation of directly driven by the interaction of matter with periodic modulation of polarization.
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●●●○ ○○○

## Slide 18: Selective excitation
Pseudospectral numerical simulations with a deterministic initial demagnetization reproduce the observed dynamics.
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●●●● ○○○
Deterministic excitation
Thermal (stochastic) excitation
K. Rockwell,et al., Phys. Rev. B 109, 180404 (2024).

## Slide 19: Summary and outlook of EUV-TG applications
Applications (so far) of EUV TG at TIMER
Bulk, surface and confined phonons
Nanoscale thermal transport
Nanoscale magnetic dynamics
All-optical magnetic switching
Short-wavelength magnons
Nanoscale polarization gratings (NPG)
Ultrafast electronic response (limited by time resolution & resonances)
Photoinduced phase transitions
Superconducting coherence length
Resonant self diffraction spectroscopy
Pulse metrology
Structured illumination microscopy (SIM)
I. Vaskivskyi et al., Nature Photonics 18, 458 (2024)
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●●●● ●○

## Slide 20: Hard X-ray TG
G2 (500nm)
G1 (1μm)
M2a (0.4°)
M2b
Si (111)
Mirror 1
M1 (0.1°)
Si (111)
Top view
Lateral view
Open questions:
Mean free path of high energy electrons allows for the excitation modulation?
Hard X-ray absorption is sparse and stochastic: Sufficiently strong Fourier component at kTG?
Complementarities to XUV-TG:
Access bulk solids & buried interfaces
Reduce periodicity down to single-digit nm
    Selectively excite charge density waves, mode couplings, quantum instabilities…
  Ultrafast (maybe as) electron dynamics ?
H. Li et al., arXiv:2506.03428
STO; EFEL=9.8 keV
Introduction Transient Grating Polarization Grating Outlook
●●●●●●●● ●●●●●● ●●●●●● ●●

## Slide 21: Many thanks to you for the attention and to…
M. Svandrlik, C. Masciovecchio, S. Lizzit, A. Locatelli
Experimental team (FERMI BLs):
F. Bencivenga, F. Capotondi, D. De Angelis, R. Mincigrucci, M. Pancaldi, E. Pedersoli, A. Simoncig, I. Lopez Quintas, and former members...
Machine physics team:
L. Giannessi, G. de Ninno, E. Allaria et al.
Laser team:
M. Danailov, G. Kurdi et al.
PADReS team:
M. Zangrando et al.
... and all the FERMI team!
A. Maznev,
K. Nelson et al.
G. Monaco et al.
J. Hastings, D. A. Reis, D. Zhu, M. Trigo et al.
M. Fuchs et al.
G. Knopp
et al.
C. Gutt et al.
S. Bonetti et al.
P. Bowlan et al.
C. von Korff Schmising et al.
R. Cucini
G. Panaccione
et al.
H. Kapteyn, M. Murnane et al.
M. Chergui
et al.
V. Giordano et al.
B. Wehninger

## Slide 22
“highly interdisciplinary journal focusing on, but not limited to, scientific studies of chemical transformation and energy materials based on photon, electron, and neutron facilities. The word “photon” here is representative of particles in modern scientific facilities.
Photon Science also reports breakthroughs in instrumentation, methodology, and big-data research with demonstrations or potential for chemistry and material science.”
Editor-in-chief:
Wanli Yang, Lawrence Berkeley National Laboratory)
Associate Editors:
Hendrik Bluhm, Fritz Haber Institute of the Max Planck Society
Laura Foglia, Elettra Sincrotrone Trieste
Hua Zhou, Argonne National Laboratory
Submission is now open!
APCs are waived for all articles submitted by December 31, 2027 if accepted after peer review.