## Slide 1: Ex situ and in situ synchrotron studies of CeO2 thin films grown by Atomic Layer Deposition
Andrea Braga – abraga@cells.es

## Slide 2: Introduction
BSc + MSc in Materials Science
University of Padua, Italy
PhD in Chemical Engineering
University of Catalonia, Barcelona, Spain
Research on catalysis for hydrogen and syngas production with synchrotron characterisation
Postdoctoral researcher at the University of Udine, Italy
Bifunctional nanomaterials for CO2 capture and conversion
Postdoctoral researcher at ALBA synchrotron, Barcelona, Spain
Development of in situ Atomic Layer Deposition characterisation and processes
Atomic Layer Deposition project at ALBA synchrotron
Development of ALD2, an in-house modular reactor for in situ and operando characterisation of ALD processes
Research focused on fundamental aspects of ALD growth, especially during the first ALD cycles
Growth of Al2O3, TiO2, CeO2, template-assisted ALD etc.
Final goal: preparation of model catalytic surface for hydrogen applications

## Slide 3: Atomic Layer Deposition
A – Precursor, tA
B – N2 purge, tB
C – co-reactant, tC
D – N2 purge, tD
Saturation curves of ALD: growth per cycle rises with precursor dose and lowers with purge time until reaching a plateau, beyond which further exposure adds no additional growth.
Thin film synthesis technique, derived from chemical vapour deposition (CVD)
The chemical reaction is split in steps with self-limiting reactions
Sub-nanometre thickness control, conformal coverage of complex geometries, high purity and uniformity, doping control
Used in semiconductor industry for high-k dielectrics, being developed for solar cells and other thin film technologies
ALD cycle
Self-limiting reactions, surface saturation
(tA)
(tB)
Surface sites available
CVD regime, precursor residues

## Slide 4: CeO2 thin films by ALD
Motivations and aims
Model catalysts for H2 production: CeO2 is a fundamental support for many catalytic reactions
Interest for high-k dielectric
CeO2 ALD processes lack characterisation
Al2O3 and TiO2 are mature, CeO2 needs more development
As of today, no thin film regime has been obtained reliably using Ce(dpdmg)3, only island growth and inhomogeneous films, no clear trend with process parameters
Track thickness with in situ XANES, mapping with ex situ XAS
Characterise the deposited Ce
Methods
CeO2 thin films are being grown on Si substrates with 2-3 nm native SiO2 layer, recipe development offline in the lab
ALD cycle consisting of a A) Ce(dpdmg)3 pulse, B) N2 purge, C) the co-reactant pulse (H2O or O2), and D) N2 purge; the timing for each step are [13, 20, 3.5, 60] seconds
Film thickness tracked at NOTOS beamline, ALBA, measuring the XANES edge jump μ of Ce L3-edge at 5700 eV every 5-10 cycles
XAS maps measured with fluorescence detection at 5800 eV of Ce signal and resolution of 10 μm at NOTOS
XPS measurements conducted in UHV in a commercial SPECS XPS

## Slide 5: XAS mapps: Ce deposition and homogeneity
Ex situ Ce L3-edge XAS maps at 5800 eV of various samples prepared in the lab with different process parameters (cycle number, substrate temperature, co-reactant, Ce precursor flow)
Standard deviation scaled linearly with XAS median intensity, coefficient of variation is constant, island growth regime.

## Slide 6: In situ XANES: tracking film thickness and chemical information
ALD Cycle
Ce3+
Ce4+
Ce3+
Ce4+
Ce L3-edge jump, direct thickness track
Raw XANES spectra collected every 5 cycles
2D XANES map, normalised spectra
Normalised XANES spectra
Ce3+ is formed during the first cycles when the film is ultrathin (or islands are very small), later CeO2 is formed.
The jump show linear ALD growth only for limited number of ALD cycles, inconsistent growth.

## Slide 7: XPS analysis: chemical information and interfaces
Sample | A | B | C
Cycles | 70 | 70 | 140
N2 flow (mL/min) | 20 | 160 | 160
Si-O-Ce3+ (%) | 5.9 | 8.4 | 13.2
Ce3+ (%) | 69.2 | 48.1 | 29.5
Total Ce (%) | 3.6 | 6.3 | 27.4
Total Ce/Si-O-Ce3+ | 0.6 | 0.7 | 2.1
Si 2p region showing Si0, SiO2, Si4+-O-Ce3+ with -1 eV shift, increasing with Ce loading.
Ce3+ is present in low-coverage films; oxidised to Ce4+ with higher loadings.
Ce3+ peaks needs to be shifted 1 eV higher compared to standard CeO2-x, probably rising from Si4+-O-Ce3+.
Total Ce/Si-O-Ce ratio indicative of island vs film or coalescence regimes.

## Slide 8: Take home message
CeO2 thin films are not obtained, and the process needs further development
XAS mapping show inhomogeneous growth and low match with process parameters
In situ XANEs showed formation of defective Ce structures and inhomogeneous growth-per-cycle regimes
XPS can track the Si-O-Ce interface and infer on the island-film regimes
Further steps: in situ XANES beamtime, operando GISAXS beamtime, systematic process optimisation, surface treatments, integration of in situ probes like quartz crystal microbalance, ellipsometry and mass spec.