## Slide 1: ReCAllTubes - Recycling Aluminium from Municipal Waste Slag for New Tube Production
Florian Brandstetter
24th September, 2026

## Slide 2: Agenda
Academic Background
Project ReCAllTubes
Current status & first results
Outlook

## Slide 3: Academic Background
PhD student since 07/2026 @ Department of Materials Science of Montanuniversität Leoben
Neutron and X-ray Team (NEXT)
Master`s degree in Materials Science in 06/2026
  Thesis: “Effect of Co and W on the Phase Transformations and Mechanical High-Temperature Properties of β-Solidifying γ-TiAl Alloys”
Project ReCAllTubes (Start 04/2026)
Muggia
Leoben
Map adapted from mappr.co, https://www.mappr.co/maps/austria/

## Slide 4: ReCAllTubes – Motivation
Primary Al production  15 t CO2 per t Al
Al as a critical raw material for the EU economy [1]
D. Raabe et al., Making sustainable aluminum by recycling scrap: The science of “dirty” alloys, Prog. Mater. Sci. 128, 2022, 100947
95%
fewer CO2 emissions
By recycling, compared to the production of packaging systems made from primary aluminum.
European Aluminium, Circular Aluminium Action Plan: A Strategy for Achieving Aluminium's Full Potential for Circular Economy by 2030, (2020)
[1] European Union, Regulation (EU) 2024/1252 establishing a framework for ensuring a secure and sustainable supply of critical raw materials, Official Journal of the European Union, (2024)

## Slide 5: ReCAllTubes – Challenges
Municipal waste incineration (MWI) slag
1
Cast Alloys (AC)
Wrought Alloys (AW)
C. Krammer, Aluminium Taschenbuch 1, 16th Edition, ISBN 978-3-410-22028-2
1xxx Al
>99% Al
AI-assisted sorting by product type (cans, tubes, coffee capsules,…) followed by alloy-class separation using X-ray fluorescence analysis (XFA).

## Slide 6: ReCAllTubes – Challenges
T
t
30s
1
2
3
Casting, rolling and billet production
Extrusion, annealing and expansion

## Slide 7: ReCAllTubes – Challenges
rolling and billet production
extrusion
annealing
expansion
casting
cracking

## Slide 8: Results – Rexx lab experiments
AW-1070A – 180s at 340°C
AW-1070A – 90s at 340°C

## Slide 9: Results – Rexx lab experiments
PCR BT2.0 – 45s at 350°C
PCR BT2.0 – 90s at 350°C

## Slide 10: Results - High-Energy X-Ray Diffraction (HEXRD)
in-situ
ex-situ
high energy materials science beamline P07
E = 102.63 keV
λ = 0.01208 nm

## Slide 11: Results – HEXRD
phases position and distribution of Debye-Scherrer rings
(residual) stresses ellipticity (peak positions), peak‘s widths
microstructure, (defects) spotty pattern, peak‘s widths
 -321
Al-111
Al-200
Al-220
Al-311
Al-222
 -413
 -530
 -600
-835
Al-400

## Slide 12: Results – HEXRD – Phases in AW-1xxx
E = 102.63 keV
λ = 0.01208 nm

## Slide 13: Results – In-situ Rexx of AW-1070A, PIR and PCR
AW-1070A
Al-111
Al-200
fast mode – time resolution 0.15 s
slow mode – time resolution 1 s
slow mode – time resolution 1 s

## Slide 14: Results – In-situ Rexx of AW-1070A, PIR and PCR
366°C
398°C
PCR BT2.0
PIR BT1.0
AW-1070A
stacking fault energy decreased by tramp and trace elements
  impurities and intermetallic phases as Rexx nucleation sites
  Over-annealing  Cracking
Al-111
Al-200

## Slide 15: Outlook – Future HEXRD experiments
Proposal for beamtime @ DESY Petra III P07 for the period of 04/2027 to 08/2027
modified dilatometer setup  rotating graphite / glassy carbon capsule as a container for melted Al samples
for in-situ investigation of (i) nucleation sequence, (ii) phase evolution (iii) microstructure evolution during an industrially relevant heat treatment straight from the melt

## Slide 16
project „ReCAllTubes“ funded by FFG, KLWPT 24/26, FTI-Initiativen 2025, Ressourcenwende 2025

## Slide 17: Rexx during continous heating
start
464°C
479°C
493°C
I
II
III
IV
I
II
III
IV
Al-111
Al-200
Al-220
Al-311
Al-222
Al-400
stacked PCR-BT2.0 sheets

## Slide 18: Melting temperatures by DSC
AW-1070 – 655.4°C
PCR BT2.0 – 648.2°C