## Slide 1: Tunable Artificial Spin Networks via Fe Coordination of Pyridyl-Based Molecules
Eidsa Brenda da Costa Ferreira¹, Isabela da Costa Tonon¹, Neeta Bisht2, Alisson Ceccatto dos Santos1, Andreas Görling2, Abner de Siervo¹
¹Department of Applied Physics, University of Campinas (UNICAMP), Campinas, Brazil
2Department of Chemistry and Pharmacy, Friedrich-Alexander-Universität Erlangen-Nürnberg, Erlangen, Germany
ebrenda@ifi.unicamp.br

## Slide 2
Surface-confined metal-organic networks (SMONs)
Dong, L. et al. Prog. Surf. Sci. 91, 101-135 (2016)

## Slide 3
Objectives and Methods
To Build and Characterize Artificial spin networks using different organic precursors
Molecule and metal
deposition
Disordered molecules
SAM
Activation
MON
Magnetic Adatom
Scanning Tunneling Microscopy (STM)
Tip
Amplifier
Tunneling current
Feedback Loop
Piezoelectric
system
Tunneling voltage
+
-
Sample
Botton-up fabrication
On-surface synthesis
X-Ray Photoelectron spectroscopy (XPS)
Low-energy Electron Diffraction (LEED)
UHV environment

## Slide 4
After 450K annealing
Au-coordinated → Fe-coordinated
networks
Honeycomb networks
TPyPB (1,3,5-tris[4-(pyridin)phenyl]benzene)
TPyPPB (1,3,5-tris[4-(pyridin)-[1,1’-biphenyl]benzene)
Vt=-0.8V ; It=-0.2nA
3-fold coordination
Fe
Pore size ~½ of TPyPPB
TPyPB on Au(111) and annealing at 450K
TPyPB on Au(111) + Fe
Au-Py
2-fold coordination
+
+
TPyPPB on Au(111) + Fe
Vt=-1.0V ; It=-0.3nA
Vt=-1.3V; It=-0.3 nA
Vt=-1.2V ; It=-0.3nA
450K
Vt=-1.2V ; It=-0.3nA
500K
Vt=-1.2V ; It=-0.3nA
~600K
Vt=-1.1V ; It=-0.2nA
450K
500K
Vt=-1.0V ; It=-0.3nA
Vt=-1.6V ; It=-0.4nA
~600K
Structural Stability up to ~600 K
Subsequent annealing → domain merging and defect reduction
TPyPPB on Au(111)
Au-Py
2-fold coordination
Vt=-1.5V; It=-0.3 nA

## Slide 5
Thank you for your attention!