## Slide 1: MONITORING OF THE ELECTRODE-ELECTROLYTE INTERFACE AND REDOX ACTIVITY IN NA-ION BATTERIES WITH CONCENTRATED AQUEOUS ELECTROLYTES
THESIS SUPERVISORS : Dr. Magali Gauthier (CEA – NIMBE, LEEL) Dr. Antonella Iadecola (CNRS – PHENIX, SOLEIL SYNCHROTRON) Dr. Jean-Blaise Brubach (SOLEIL SYNCHROTRON)
PRESENTED BY HARINI MOHANRAAJ – 24/09/2026 School on Synchrotron Radiation: Fundamentals, Methods and Applications

## Slide 2: 1. Na-ion Aqueous Batteries with « Water-In-Salt Electrolytes »
Water H2O
Sodium-based salt (NaClO4)
Lithium-based salt
Li-ion batteries in all electrical devices
ELECTROLYTE
Flammable organic solvent
Na-ion Aqueous batteries
Sustainable and low-cost
However, the electrochemical stability window (ESW) of water is narrow….

## Slide 3: 1. Na-ion Aqueous Batteries with « Water-In-Salt Electrolytes »
m, molality : moles per kg of water
17 m = 68%w. of NaClO4 + 32%w. of water
Highly concentrated electrolytes for widening the ESW (2015) [1]
Modification of the electrolyte structure with increasing salt concentration, associated with a reduction in free water molecules
High concentration
SEI = Solid Electrolyte Interphase
Determines long-term stability and performance
OBJECTIVE : To better understand the formation and evolution of the SEI in aqueous Na-ion batteries using operando infrared and X-ray spectroscopy
[1] L. Suo et al., Science, 2015, 350, 938-943.

## Slide 4: 2. Objectives and methods
OBJECTIVE : To better understand the formation and evolution of the SEI in aqueous Na-ion batteries using operando infrared and X-ray spectroscopy
REDOX ACTIVITY AND STABILITY OF AQUEOUS CELLS
Aqueous vs. organic comparison
Study of various negative electrodes, various cycling parameters
FOURIER-TRANSFORM INFRARED SPECTROSCOPY (FT-IR) AND X-RAY ABSORPTION (XAS)
FT-IR : evolution of water (solvation), interfacial layers
XAS : local structure and oxidation state at V et Ti K edge
Synchrotron for IR: water absorption and study of low-frequency vibrations (Na+, evolution due to changes in oxidation states)

## Slide 5: 3. Redox activity and electrochemical performances
AQUEOUS
ORGANIC
Hypotheses regarding the mechanisms responsible for the drop in capacity
Intercalation of H3O+
No SEI formed  surface reactions
[2]
[2] Huang et al., Nat. Commun. (2024)
 | Storage mechanism
NVP Na3V2(PO4)3 | Insertion/extraction of Na⁺ (V3+/V2+)
NTP NaTi2(PO4)3 | Insertion/extraction of Na⁺ (Ti4+/Ti3+)

## Slide 6: 4. FTIR operando measurements
CHARGE
DISCHARGE
Region A: Rotation of PO4 groups (T’(PO4) and R'(PO4))
Region B: V–O bonds
Region C: ν4 deformation of PO4 groups

## Slide 7: Thank you for your attention!