## Slide 1: UV-VUV excited thermally-stimulated and delayed luminescence in Ce-doped scintillating crystals
Pietro Moiraghi, Francesca Cova, Vittoria Vigorito, Alessandra Ronchi, Alberto Paleari, Mauro Fasoli, Roberto Lorenzi
University of Milano-Bicocca
Department of Materials Science
“Gilberto Vlaic” XVIII School on Synchrotron Radiation: Fundamentals, Methods and Applications – Muggia, 24th September 2026

## Slide 2: Charge trapping and release
Thermally stimulated or delayed luminescence
Detrapping
Prompt luminescence
Luminescence centre
Valence band
Conduction band
Electron trap
Excitation
Excitation
Free charge carriers
Recombination (prompt luminescence)
Charge trapping
Detrapping and recombination
Heat/time
10–10 – 10–7 s
10–2 – 103 s

## Slide 3: Kinetics and trap parameters
Thermally stimulated luminescence (TSL)
1st order kinetics
2nd order kinetics
Rate equation
Phosphorescence
TSL equation with β (linear ramp)
Peak position
Variable heating rate (VHR) method
Arrhenius plot (from phosphorescence data)
Estimation of trap parameters (, )
Time
T
I(t)
0
0
n
n0
Slope = β
TM
Number of trapped charges
TSL glow curve
Heating ramp
Heat
S. W. S. McKeever, Thermoluminescence of Solids (Cambridge University Press, Cambridge, 1985)

## Slide 4: Materials
5d1
5d2
5d3
5d4
5d5
Eg
5d1
5d2
5d3
5d4
5d5
Eg
5d1
5d2
5d3
5d4
5d5
Eg
Gd3+
Defect
Ce:YAG
Ce:YAP
Ce:GGAG
Eg
Ce:YAG
Ce:YAP
4f1 (split)
5d1
5d2
5d3
5d4
5d5
Ce:GGAG
?
Photoluminescence
Absolute energies and spacing of the 4f1 and 5d levels
Location of the Ce levels in the energy gap of the host crystals
Ce-doped scintillating crystals:
YAG (Y3Al5O12) → garnet structure, Ce3+ substitutes Y3+ in the dodecahedral site
YAP (YAlO3) → perovskite structure, Ce3+ substitutes Y3+ in the A site
GGAG (Gd3(Ga,Al)5O12) → garnet structure, Ce3+ substitutes Gd3+ in the dodecahedral site

## Slide 5: Results
6.7 eV
7.8 eV
6.3 eV
4f1
(split)
5d1
5d2
5d3
5d4
5d5
Ce:YAG
Ce:YAP
Ce:GGAG
TSL?
×
×
×
×
×
✓
✓
✓
✓
✓
✓
✓
✓
✓
×
TSL?
TSL?
Ce:YAP
Trap 1
Trap 2
VHR
Arrhenius plot
E1 = 0.18 eV
E2 = 0.30 eV
E1 = 0.16 eV
E2 = 0.11 eV

## Slide 6: Thank you for your attention!
DESY PETRA III beamline P66 Superlumi endstation proposal number I-20250130EC
Funding from the Italian Ministry of Research under the project Luminance of the PRIN2022 program (Grant Agreement 2022E42PMA), funded by the European Union – Next Generation EU
Synchrotron light (DESY, Hamburg): Dr. Aleksey Kotlov,
Dr. Yevheniia Smortsova
Campaign: Prof. Alberto Paleari, Prof. Roberto Lorenzi, Dr. Francesca Cova,
Dr. Alessandra Ronchi, Vittoria Vigorito, Pietro Moiraghi
“Gilberto Vlaic” XVIII School on Synchrotron Radiation: Fundamentals, Methods and Applications – Muggia, 24th September 2026 Pietro Moiraghi
Synchrotron radiation is a useful tuneable light source for thermoluminescence and phosphorescence measurements.
Changing excitation energy yielded information on energy levels within and above the gap and on the defects responsible for the peaks observed in the glow curves.
Synchrotron radiation allows the investigation of trapping and detrapping mechanisms for energy levels inside the conduction band, which would not be accessible with lab-scale UV-vis excitation.