## Slide 1
Bridging UV and soft X-ray excitation in luminescent materials for scintillation
V. Vigorito1, R. Lorenzi1, A. Paleari1, A. Ronchi1, A. Erroi1, F. Cova1
1Department of Materials Science, University of Milano-Bicocca, Milan, Italy
“Gilberto Vlaic” XVIII School on Synchrotron Radiation: Fundamentals, Methods and Applications
24 September 2026 - Muggia (Italy)

## Slide 2
Scintillation
A scintillator is a material that absorbs high-energy radiation and re-emits part of that absorbed energy as light, typically in the visible or near-visible range
Scintillating material
X-rays, γ-rays, neutrons, electrons and α particles
Classes of scintillators
Energy
Conduction band
Ionizing radiation
Deep hole
Hot electron
2
Transfer
3
1
Valence band
Core levels
Luminescence
INORGANIC
ORGANIC
LIQUID
NANOCRYSTALS
Absorption and multiplication
Carrier migration
Relaxation and emission
Dujardin C. Tech. Ingénieur EE6347 (2018)

## Slide 3
Material
LEAD HALIDE PEROVSKITES
General formula: ABX3
A: Large monovalent cation ()
B: Smaller divalent metal cation
()
X: Halide anion ()
By varying the halide ratios in the colloidal nanocrystal solution, the PL can be tuned across the entire visible spectral range
G. Nedelcu et al. Nano Lett. 15,5635−5640 (2015)
Q. A. Akkerman et al. Nature Materials, 17, 394–405 (2018)

## Slide 4
Material
LEAD HALIDE PEROVSKITES
By varying the halide ratios in the colloidal nanocrystal solution, the PL can be tuned across the entire visible spectral range
CsPbBr3
Hot‑injection synthesis rapidly mixes precursors into a hot solvent, inducing immediate nucleation of perovskite nanocrystals.
Cova F et al. Nano Lett 24, 905–913 (2024)
G. Nedelcu et al. Nano Lett. 15,5635−5640 (2015)
Q. A. Akkerman et al. Nature Materials, 17, 394–405 (2018)
General formula: ABX3
A: Large monovalent cation ()
B: Smaller divalent metal cation
()
X: Halide anion ()

## Slide 5
Bridging the excitation gap
RL
PL
A difference in emission behavior when the material is excited optically versus when it's excited by ionizing radiation is observed
Exc energy
Exc energy 20 keV

## Slide 6
Bridging the excitation gap
RL
PL
A difference in emission behavior when the material is excited optically versus when it's excited by ionizing radiation is observed
Synchrotron light can be used to bridge the gap in the excitation photon energies between UV/Vis lamps and x-ray tubes routinely used in labs
Radioluminescence
Exc energy
Exc energy 20 keV

## Slide 7
Bridging the excitation gap
RL
PL
RL maximum (for reference)
Synchrotron light can be used to bridge the gap in the excitation photon energies between UV/Vis lamps and x-ray tubes routinely used in labs
A difference in emission behavior when the material is excited optically versus when it's excited by ionizing radiation is observed
Radioluminescence
Exc energy
Exc energy 20 keV

## Slide 8
Aknowledgments
Synchrotron campaigns: Dr. Francesca Cova, Prof. Roberto Lorenzi, Prof. Alberto Paleari, Prof. Franco Meinardi, Dr. Andrea Erroi, Pietro Moiraghi, Dr. Alessandra Ronchi
Synchrotron light from DESY, Hamburg, Germany: Dr. Aleksei Kotlov, Yevheniia Smortsova
Synchrotron light from MAXIV, Lund, Sweden: Dr. Antti Kivimäki, Dr. Kirill Chernenko
MAX IV FinEstBeAMS beamline, proposal umber 20241473
Thank you for your attention